## Slide 1
Robert J. Frosch, PhD, PE, FACI, FASCE
Eric T. Fleet
Rebecca Glucksman
Development and splice lengths for high-strength reinforcement
Volume I: general bar development

## Slide 2
Context
Testing and Results
Bond Modeling - Unconfined
Bond Modeling - Confined
Conclusions
outline

## Slide 3: 1. context

## Slide 4
Background:
General
Standard yield strength for reinforcing bars = 60 ksi
High-strength steels becoming commercially available (Gr. 100)
  ASTM A615, A1035 (MMFX)
ACI 318 was developed considering Grade 60 reinforcement
Applied Technology Council (ATC-115) – roadmap for the adoption of high-strength reinforcement
1. Context

## Slide 5
Objective and Scope
Evaluate the development of high-strength reinforcing steel
Establish a design expression for the development of high-strength reinforcing steel
Glucksman 2018:
  Failure Modes
  Effect of Splice Length
  Confinement Pressure
  Transverse Reinforcement Grade
Fleet 2019:
  Bar Development in Slabs
  Effect of High-Strength Concrete
  ASTM A615 vs. A1035
  Confinement Location in Splice
1. Context

## Slide 6: 2. Testing and results

## Slide 7
Specimen Design – Beams
2. Testing and Results
Unconfined Beams
  ASTM A615 & A1035 longitudinal bars
  Normal-strength concrete and high-strength concrete
  40db < Ls < 120db

## Slide 8
Specimen Design – Beams
2. Testing and Results
Test Setup Dimensions

## Slide 9
Splitting failure only
  Brittle, explosive
ASTM A1035 vs. ASTM A615
  No difference
  Linear-Elastic region
beams – unconfined Results
2. Testing and Results
U-60-10
U-40-5-X

## Slide 10
The concrete contribution toward increasing bar stress is better estimated by the quarter root of the ratio between high-strength concrete (HSC) and normal-strength concrete (NSC) when compared to the square root
  18% for 40db
  17% for 60db
beams – unconfined Results
2. Testing and Results
Effect of High Strength Concrete

## Slide 11
beams – unconfined Results
2. Testing and Results
All unconfined beams failed by splitting of the concrete
A1035

## Slide 12
Confined Beams
  ASTM A615 longitudinal bars
  No. 3 & 4 Stirrups, Grade 60 & 100
  Normal-strength concrete and high-strength concrete
  40db < Ls < 80db
Specimen Design – Beams
2. Testing and Results

## Slide 13
Specimen Design – Beams
2. Testing and Results
Test Setup Dimensions

## Slide 14
Longitudinal cracking present above splice, regardless of failure mode
Splitting and flexural failures occurred
  Transition in failure mode by increasing confinement pressure
  For example, C3/60-50-5-150 failed in splitting while C3/60-50-5-200 failed in flexure at the north support
beams – confined Results
2. Testing and Results
C3/60-50-5-200
C3/60-50-5-150

## Slide 15
Effect of splice length on bar stress is best represented by the square root (Glucksman 2018)
beams – confined Results
2. Testing and Results
Chart: ls (in.)
| 40 | 60 | 40
Below Elastic Limit | 58.8808 | 69.3193 | 65.9864
Beyond Elastic Limit | 84.0428 | 89.715 | 103.5735 | 105.0937 | 104.891

## Slide 16
As confinement pressure increases, bar stress increases until a flexural failure is induced, after which additional confinement pressure has no effect. (Glucksman 2018)
beams – confined Results
2. Testing and Results
Chart: Effective Pressure (psi)
| 50 | 100
40db | 81.7959 | 91.6763
60db | 103.2986 | 110.4966 | 109.4209
Flexural Failure
40db
60db

## Slide 17
2. Testing and Results
The distributed transverse reinforcement ratio, , compares the transverse reinforcement area of one confining element to the area of the surrounding concrete that element confines. This provides a way to describe transverse reinforcement strength independent of the yield strength of the transverse steel, .
Distributed transverse reinforcement ratio

## Slide 18
2. Testing and Results
Distributed transverse reinforcement ratio
When compared to normalized bar stress, it is difficult to determine an overall trend from the data in this testing program
Larger spacing, s
Smaller spacing, s

## Slide 19
2. Testing and Results
C3/60/2-40-10-25
C3/60/2-40-10-50
C3/60/3-40-10-50
Distributed transverse reinforcement ratio
Two inner stirrups appear to be slightly less effective in confining the longitudinal bars than two outer stirrups

## Slide 20
Sim (2014)
2. Testing and Results
Research from Sim (2014) indicates that stirrups placed in the middle of the splice are ineffective in resisting longitudinal bar stress, while stirrups placed near the ends of the splice are highly effective.
Distributed transverse reinforcement ratio

## Slide 21
Specimen Design – Slabs
2. Testing and Results
Slabs
  ASTM A615 longitudinal bars
  5000 psi concrete
  40db < Ls < 100db

## Slide 22
Specimen Design – Slabs
2. Testing and Results
Test Setup Dimensions

## Slide 23
Longitudinal cracking present above all splices, regardless of failure mode
Slabs – Results
2. Testing and Results
37.5 in. Splice (S-60-5)

## Slide 24
A615 Grade 100 bars fully developed their strength
  Transition of failure mode
Slabs – Results
2. Testing and Results
25 in. Splice
S-40-5
S-80-5
50 in. Splice

## Slide 25: 3. Bond Modeling - Unconfined

## Slide 26
Bond modeling
Concrete Contribution (Unconfined)
Bar Stress
Dependent on Cover?
Darwin et al. 1996
Zuo and Darwin 2000
Canbay and Frosch 2005
Pay 2005
Sim 2014
Glucksman 2018
Canbay and Frosch 2005
Pay 2005
Sim 2014
Glucksman 2018
3. bond modeling - unconfined

## Slide 27
Unconfined database
  ACI 408 Database 10-2001
    132 of the original 192
    Bottom-cast, uncoated bars
    Exclusion criteria:
  Later Testing
    77 additional specimens
      Seliem et al. 2009
      Sim 2014
      Glucksman 2018
      Fleet 2019
      Others
  Total: 209 Unconfined Beams
    167 with ASTM A615 Bars
    42 with ASTM A1035 Bars
3. bond modeling - unconfined

## Slide 28
Cover modifier options
3. bond modeling - unconfined
Options
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
8 | 
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
8 | 

## Slide 29
Cover modifier options
3. bond modeling - unconfined
Options
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
8 | 
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
8 | 

## Slide 30
Cover modifier options
3. bond modeling - unconfined
Options
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
8 | 
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
8 | 

## Slide 31
Nonlinear regression analysis
3. bond modeling - unconfined
:

## Slide 32
Comparison of unconfined database to aci 318
  ACI 318-14
  Proposed Equation
3. bond modeling - unconfined
Avg. = 1.23
Std. Dev. = 0.405
COV = 0.328
Avg. = 1.00
Std. Dev. = 0.155
COV = 0.155
0

## Slide 33: 4. bond modeling - confined

## Slide 34
Bond modeling
Concrete (Unconfined)
Transverse Steel (Confined)
Bar Stress
4. bond modeling - confined
Resistance force of 1 stirrup:
Total Resistance Force:

## Slide 35
Bond modeling
4. bond modeling - confined
(Canbay and Frosch, 2005)
  Stress in each stirrup is unequal due to nonuniform bond stress distribution in the longitudinal bars.
  Question: How can these regions where stirrups have varying degrees of effectiveness be represented by a model?

## Slide 36
confinement model
4. bond modeling - confined
Splice Centerline
Stirrups
50% Effective
  Segmented, nonlinear model with defined distances a and b

## Slide 37
confinement model
Model A
Model B
Model C
Model D
4. bond modeling - confined
  Potential models considered

## Slide 38
confinement model
4. bond modeling - confined
Splice Centerline
Model D
  Model D was selected for the analysis to determine 𝑁𝑠,𝑒𝑓𝑓

## Slide 39
Stirrup Spacing Options
  Large range of possible stirrup spacings
    Based on number of stirrups (Ns) and the splice length (ls)
    Equal spacing and symmetric about middle of splice
    Range of spacings is large for small Ns, but small for large Ns
4. bond modeling - confined
3-Stirrup Example:

## Slide 40
Percent Contribution
  Large range of possible k values
    Based on number of stirrups (Ns), a given splice length, and selected spacing
    Variability results from large range of possible stirrup spacings
    k converges on 50% as Ns increases for all spacings
4. bond modeling - confined
50%

## Slide 41
Percent Contribution
4. bond modeling - confined
  Comparison of tested specimens at different stirrup spacings
    Circles indicate beams tested in Series IV (Glucksman 2018)
    Squares indicate beams tested in Series VI and VII (Fleet 2019)
    Triangles indicate beams tested by Sim (2014)
Glucksman 2018
Fleet 2019

## Slide 42
Confinement term
4. bond modeling - confined

## Slide 43
Confinement term
4. bond modeling - confined
Force in 1 Splice (1 bar)
Force in 1 Stirrup
Number of Effective Stirrups

## Slide 44
confined database
  ACI 408 Database 10-2001
    266 of the original 286 beams
    Bottom-cast, uncoated bars
    Exclusion criteria:
      1 stirrup
      1 splice
  Later Testing
    56 additional specimens
      Seliem et al. 2009
      Sim 2014
      Glucksman 2018
      Fleet 2019
  Total: 322 Confined Beams
    281 with ASTM A615 bars
    41 with ASTM A1035 bars
    85 reached yield before failure
4. bond modeling - confined

## Slide 45
Confined pair database
4. bond modeling - confined
Question: How can an appropriate value for k be confirmed from previous testing data?
Answer:
  Identified 101 beam pairs in the confined beam database
    1 unconfined beam and 1 identical beam containing confinement
  Compared with by varying k

## Slide 46
Confined pair database
4. bond modeling - confined
  Trendline coefficient is greater than 1 when k = 0.40

## Slide 47
Confined pair database
4. bond modeling - confined
  Trendline coefficient is slightly greater than 1 when k = 0.45

## Slide 48
Confined pair database
4. bond modeling - confined
  Trendline coefficient is nearly 1 when k = 0.50

## Slide 49
Confined pair database
4. bond modeling - confined
  Trendline coefficient is less than 1 when k = 0.55

## Slide 50
Full equation
4. bond modeling - confined

## Slide 51
Comparison of confined Database to aci 318
  ACI 318-14
  Proposed Equation
4. bond modeling - confined
Avg. = 1.30
Std. Dev. = 0.300
COV = 0.230
Avg. = 0.94
Std. Dev. = 0.129
COV = 0.136

## Slide 52: 5. conclusions

## Slide 53
Findings
5. Conclusions
Confined Beams:
Confinement location matters
Confinement for short splices can lead to flexural failure
A increases, increases
Unconfined Beams:
Splitting failure only
is best represented by
No difference between ASTM A615 and A1035 longitudinal bars
Slabs:
Full bar strength achieved when

## Slide 54
5. Conclusions
Bond model - Unconfined
Nonlinear Regression Analysis

## Slide 55
5. Conclusions
Bond model - COnfined
Effective Confinement Model

## Slide 56
Design expression
5. Conclusions
  Side clear cover (beams)
  ½ clear bar spacing (slabs)
where:

## Slide 57
Design expression
5. Conclusions
The cover modifier can be taken as 1.0 when designing members for practical use to avoid complication in the calculation
A cover modifier of 1.0 is slightly conservative for beams, but too conservative for slab design due to typical bar sizes and large bar spacings

## Slide 58
The following concepts are considered future research topics that will further our understanding of bond behavior
Future research
5. Conclusions

## Slide 59
Nonlinear Behavior of ASTM A1035 (MMFX)
  Effect on bond as bars approach yield strength
Future research
5. Conclusions

## Slide 60
Future research
5. Conclusions
Stirrup Configuration
  Stirrup concentration at distinct points along the splice length

## Slide 61
Future research
5. Conclusions
Continued investigation into the linearity of
  Linear or nonlinear relationship?

## Slide 62
Future research
5. Conclusions
Continuous Nonlinear Confinement Model
  Better representation of bond stress distribution